Copyright 2015 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 042000 - UNIT MASONRY

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

<Double click here to submit questions, comments, or suggested edits to this section.>

      - SUMMARY

        - Section Includes:

          - Concrete masonry units.

          - Steel reinforcing bars.

      - ALLOWANCES

Retain products and work included in this Section that are covered by cash or quantity allowance. Do not include amounts. Insert descriptions of items in Part 2 or 3 to provide information affecting the cost of the Work that is not included under the allowance. Revise paragraph below if allowances are required for other types of masonry units. Include separate allowances for special shapes if required.

        - Face brick is part of the Face Brick Allowance.

      - DEFINITIONS

Retain terms that remain after this Section has been edited.

        - CMU(s): Concrete masonry unit(s).

        - Reinforced Masonry: Masonry containing reinforcing steel in grouted cells.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

        - Shop Drawings: For reinforcing steel. Detail bending, lap lengths, and placement of unit masonry reinforcing bars. Comply with ACI 315.

        - Samples for Verification: For each type and color of exposed masonry unit and colored mortar.

      - INFORMATIONAL SUBMITTALS

Usually retain "Material Certificates" Paragraph below. Material certificates are required for all masonry constructed according to TMS 402/ACI 530/ASCE 5. Retain second option if required by authorities having jurisdiction or if the added assurance of quality that test reports provide is desired.

        - Material Certificates: For each type and size of product. For masonry units, include data on material properties and material test reports substantiating compliance with requirements.

        - Mix Designs: For each type of mortar and grout. Include description of type and proportions of ingredients.

          - Include test reports for mortar mixes required to comply with property specification. Test according to ASTM C 109/C 109M for compressive strength, ASTM C 1506 for water retention, and ASTM C 91/C 91M for air content.

          - Include test reports, according to ASTM C 1019, for grout mixes required to comply with compressive strength requirement.

      - FIELD CONDITIONS

        - Cold-Weather Requirements: Do not use frozen materials or materials mixed or coated with ice or frost. Do not build on frozen substrates. Remove and replace unit masonry damaged by frost or by freezing conditions. Comply with cold-weather construction requirements contained in TMS 602/ACI 530.1/ASCE 6.

        - Hot-Weather Requirements: Comply with hot-weather construction requirements contained in TMS 602/ACI 530.1/ASCE 6.

- PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

      - UNIT MASONRY, GENERAL

        - Masonry Standard: Comply with TMS 602/ACI 530.1/ASCE 6, except as modified by requirements in the Contract Documents.

        - Defective Units: Referenced masonry unit standards may allow a certain percentage of units to contain chips, cracks, or other defects exceeding limits stated. Do not use units where such defects are exposed in the completed Work.

See BIA Technical Notes 16B and NCMA TEK 7-3 for information on determining fire-resistance ratings of masonry walls.

        - Fire-Resistance Ratings: Comply with requirements for fire-resistance-rated assembly designs indicated.

Retain subparagraph below if required by authorities having jurisdiction.

          - Where fire-resistance-rated construction is indicated, units shall be listed and labeled by a qualified testing agency acceptable to authorities having jurisdiction.

      - CONCRETE MASONRY UNITS

        - Shapes: Provide shapes indicated and as follows, with exposed surfaces matching exposed faces of adjacent units unless otherwise indicated.

          - Provide special shapes for lintels, corners, jambs, sashes, movement joints, headers, bonding, and other special conditions.

Retain "Integral Water Repellent" Paragraph below for increased water resistance of units if required. If retaining, also retain water-repellent mortar admixture.

        - Integral Water Repellent: Provide units made with integral water repellent for exposed units and where indicated.

Copy and revise "CMUs" Paragraph below for nonload-bearing CMUs (changing ASTM C 90 to ASTM C 129) if needed; they are not usually an inventory item and may have to be ordered in large quantities. Indicate load-bearing and nonload-bearing units on Drawings if both are specified.

        - CMUs: ASTM C 90.

Usually retain "Unit Compressive Strength" Subparagraph below only for masonry designed by analytical methods; delete if compressive strength specified in ASTM C 90, which is 1900 psi (13.1 MPa), is acceptable. See the Evaluations.

          - Unit Compressive Strength: Provide units with minimum average net-area compressive strength of 2000 psi..

Retain one of first three options in "Density Classification" Subparagraph below, or delete subparagraph for Contractor's option. Retain last option below for default requirement if using more than one weight. See the Evaluations.

          - Density Classification: Normal weight.

Concrete building bricks are often used to adjust dimensions in CMU construction.

      - MORTAR AND GROUT MATERIALS

Coordinate requirements in this article with those in "Mortar and Grout Mixes" Article.

        - Portland Cement: ASTM C 150/C 150M, Type I or II, except Type III may be used for cold-weather construction. Provide natural color or white cement as required to produce mortar color indicated.

        - Hydrated Lime: ASTM C 207, Type S.

Mix in "Portland Cement-Lime Mix" Paragraph below allows better control of color than job-mixed, portland cement-lime mortar. If retaining below, also retain "Portland Cement" and "Hydrated Lime" paragraphs above.

        - Portland Cement-Lime Mix: Packaged blend of portland cement and hydrated lime containing no other ingredients.

        - Masonry Cement: ASTM C 91/C 91M.

Retain "Mortar Pigments" Paragraph below for colored cement or for pigments added at Project site.

        - Mortar Pigments: Natural and synthetic iron oxides and chromium oxides, compounded for use in mortar mixes and complying with ASTM C 979/C 979M. Use only pigments with a record of satisfactory performance in masonry mortar.

Mixes in "Colored Cement Products" Paragraph below allow better control of color than job-mixed colored mortar. If retaining, also retain paragraphs above that specify materials included in the mixes retained below.

        - Colored Cement Products: Packaged blend made from portland cement and hydrated lime or [masonry cement and mortar pigments, all complying with specified requirements, and containing no other ingredients.

        - Aggregate for Mortar: ASTM C 144.

          - For joints less than 1/4 inch (6 mm) thick, use aggregate graded with 100 percent passing the No. 16 (1.18-mm) sieve.

          - White-Mortar Aggregates: Natural white sand or crushed white stone.

          - Colored-Mortar Aggregates: Natural sand or crushed stone of color necessary to produce required mortar color.

        - Aggregate for Grout: ASTM C 404.

Delete "Epoxy Pointing Mortar" Paragraph below if not needed for pre-faced CMUs, glazed brick, or glazed structural clay facing tile.

        - Epoxy Pointing Mortar: ASTM C 395, epoxy-resin-based material formulated for use as pointing mortar for glazed or pre-faced masonry units (and approved for such use by manufacturer of units); in color indicated or, if not otherwise indicated, as selected by Architect from manufacturer's colors.

"Cold-Weather Admixture" Paragraph below is an example of a requirement for a concrete admixture often used in cold weather as an antifreeze. Appendix X1 in ASTM C 270 and BIA generally recommend not using admixtures unless they are known to have no adverse effects. Before approving the use of cold-weather admixtures, verify their acceptability by laboratory testing with mortar mix used.

        - Cold-Weather Admixture: Nonchloride, noncorrosive, accelerating admixture complying with ASTM C 494/C 494M, Type C, and recommended by manufacturer for use in masonry mortar of composition indicated.

Retain "Water-Repellent Admixture" Paragraph below if integral water repellent is used in CMUs.

        - Water-Repellent Admixture: Liquid water-repellent mortar admixture intended for use with CMUs containing integral water repellent from same manufacturer.

        - Water: Potable.

      - REINFORCEMENT

Retain "Uncoated-Steel Reinforcing Bars" Paragraph below for reinforcing bars in grouted cells. Revise if another grade of steel is required. Revise to specify epoxy-coated, stainless-steel, or galvanized bars if required.

        - Uncoated-Steel Reinforcing Bars: ASTM A 615/A 615M or ASTM A 996/A 996M, Grade 60 (Grade 420).

Standard in "Masonry-Joint Reinforcement, General" Paragraph below includes requirements for mill-galvanized carbon steel, hot-dip galvanized carbon steel, and stainless steel. Specifying these materials separately is unnecessary.

        - Masonry-Joint Reinforcement, General: ASTM A 951/A 951M.

Mill-galvanized coating is not as thick as hot-dip galvanized coating. According to ASTM A 951/A 951M, mill-galvanized coating may be applied to wire before fabricating, but hot-dip galvanized coating must be applied after fabricating.

          - Interior Walls: Hot-dip galvanized carbon steel.

          - Exterior Walls: Hot-dip galvanized carbon steel.

          - Spacing of Cross Rods, Tabs, and Cross Ties: Not more than 16 inches (407 mm) o.c.

          - Provide in lengths of not less than 10 feet (3 m).

Where grouted cells contain reinforcing bars, ladder-type reinforcement works better than truss type.

      - TIES AND ANCHORS

        - General: Ties and anchors shall extend at least 1-1/2 inches (38 mm) into veneer but with at least a 5/8-inch (16-mm) cover on outside face.

        - Materials: Provide ties and anchors specified in this article that are made from materials that comply with the following unless otherwise indicated:

Retain subparagraphs below only for those materials referenced in subsequent paragraphs.

          - Hot-Dip Galvanized, Carbon-Steel Wire: ASTM A 82/A 82M, with ASTM A 153/A 153M, Class B-2 coating.

          - Steel Sheet, Galvanized after Fabrication: ASTM A 1008/A 1008M, Commercial Steel, with ASTM A 153/A 153M, Class B coating.

Retain "Steel Plates, Shapes, and Bars" Subparagraph below if required for rigid anchors.

          - Steel Plates, Shapes, and Bars: ASTM A 36/A 36M.

        - Rigid Anchors: Fabricate from steel bars 1-1/2 inches (38 mm) wide by 1/4 inch (6.35 mm) thick by 24 inches (610 mm) long, with ends turned up 2 inches (51 mm) or with cross pins unless otherwise indicated.

Retain one of three options in "Corrosion Protection" Subparagraph below. Rigid anchors may not be fully embedded in mortar or grout and therefore require a coating for corrosion protection. TMS 602/ACI 530.1/ASCE 6 requires hot-dip galvanized or epoxy coating.

          - Corrosion Protection: Epoxy coating 0.020 inch (0.51 mm) thick.

      - EMBEDDED FLASHING MATERIALS

See the Evaluations for discussion of flashing materials before revising this article.

Coordinate "Metal Flashing" Paragraph below with Section 076200 "Sheet Metal Flashing and Trim." Metal through-wall flashing is included in that Section.

        - Metal Flashing: Provide metal flashing complying with Section 076200 "Sheet Metal Flashing and Trim" and as follows:

Retain one or both of first two subparagraphs below for use with flexible flashing if required. See the Evaluations.

          - Fabricate metal drip edges from stainless steel. Extend at least 3 inches (76 mm) into wall and 1/2 inch (13 mm) out from wall, with outer edge bent down 30 degrees[ and hemmed].

          - Fabricate metal sealant stops from stainless steel. Extend at least 3 inches (76 mm) into wall and out to exterior face of wall. At exterior face of wall, bend metal back on itself for 3/4 inch (19 mm) and down into joint 1/4 inch (6 mm) to form a stop for retaining sealant backer rod.

          - Fabricate metal expansion-joint strips from [stainless steel] [copper] to shapes indicated.

Delete "Flexible Flashing" Paragraph below if only metal flashing is allowed. If concealed metal flashing is required at certain locations, indicate those locations on Drawings or revise paragraph.

        - Adhesives, Primers, and Seam Tapes for Flashings: Flashing manufacturer's standard products or products recommended by flashing manufacturer for bonding flashing sheets to each other and to substrates.

      - MISCELLANEOUS MASONRY ACCESSORIES

        - Compressible Filler: Premolded filler strips complying with ASTM D 1056, Grade 2A1; compressible up to 35 percent; of width and thickness indicated; formulated from neoprene urethane or PVC.

        - Preformed Control-Joint Gaskets: Made from styrene-butadiene-rubber compound, complying with ASTM D 2000, Designation M2AA-805 or PVC, complying with ASTM D 2287, Type PVC-65406 and designed to fit standard sash block and to maintain lateral stability in masonry wall; size and configuration as indicated.

        - Bond-Breaker Strips: Asphalt-saturated felt complying with ASTM D 226/D 226M, Type I (No. 15 asphalt felt).

      - MASONRY-CELL FILL

        - Solid grout all cells.

      - MORTAR AND GROUT MIXES

        - General: Do not use admixtures, including pigments, air-entraining agents, accelerators, retarders, water-repellent agents, antifreeze compounds, or other admixtures unless otherwise indicated.

          - Do not use calcium chloride in mortar or grout.

Retain one or more of first three subparagraphs below to indicate acceptable mortar types.

          - Use portland cement-lime mortar unless otherwise indicated.

          - For exterior masonry, use portland cement-lime mortar.

          - For reinforced masonry, use portland cement-lime mortar.

          - Add cold-weather admixture (if used) at same rate for all mortar that will be exposed to view, regardless of weather conditions, to ensure that mortar color is consistent.

Preblended, dry mortar mix can help ensure uniformity, but is inappropriate for small projects.

        - Preblended, Dry Mortar Mix: Furnish dry mortar ingredients in form of a preblended mix. Measure quantities by weight to ensure accurate proportions, and thoroughly blend ingredients before delivering to Project site.

        - Mortar for Unit Masonry: Comply with ASTM C 270. Provide the following types of mortar for applications stated unless another type is indicated

Before retaining mortar types in subparagraphs below, see Appendix X1 in ASTM C 270 and BIA Technical Notes 8A and 8B for recommendations; coordinate with requirements for masonry compressive strengths.

          - For reinforced masonry, use Type S.

        - Grout for Unit Masonry: Comply with ASTM C 476.

          - Use grout of type indicated or, if not otherwise indicated, of type (fine or coarse) that will comply with TMS 602/ACI 530.1/ASCE 6 for dimensions of grout spaces and pour height.

          - Proportion grout in accordance with ASTM C 476, paragraph 4.2.2 for specified 28-day compressive strength indicated, but not less than 2000 psi (14 MPa).

          - Provide grout with a slump of 8 to 11 inches as measured according to ASTM C 143/C 143M.

        - Epoxy Pointing Mortar: Mix epoxy pointing mortar to comply with mortar manufacturer's written instructions.

          - Application: Use epoxy pointing mortar for exposed mortar joints with the following units:

            - Pre-faced CMUs.

            - Glazed structural clay facing tile.

- EXECUTION

      - INSTALLATION, GENERAL

        - Use full-size units without cutting if possible. If cutting is required to provide a continuous pattern or to fit adjoining construction, cut units with motor-driven saws; provide clean, sharp, unchipped edges. Allow units to dry before laying unless wetting of units is specified. Install cut units with cut surfaces and, where possible, cut edges concealed.

        - Select and arrange units for exposed unit masonry to produce a uniform blend of colors and textures. Mix units from several pallets or cubes as they are placed.

Retain "Wetting of Brick" Paragraph below for high-suction brick. A simple test to determine if wetting is required consists of drawing a circle the size of a quarter on a brick and placing 20 drops of water in the circle; if water is absorbed within 1-1/2 minutes, the brick requires wetting.

        - Wetting of Brick: Wet brick before laying if initial rate of absorption exceeds 30 g/30 sq. in. (30 g/194 sq. cm) per minute when tested according to ASTM C 67. Allow units to absorb water so they are damp but not wet at time of laying.

      - TOLERANCES

        - Dimensions and Locations of Elements:

          - For dimensions in cross section or elevation, do not vary by more than plus 1/2 inch (12 mm) or minus 1/4 inch (6 mm).

          - For location of elements in plan, do not vary from that indicated by more than plus or minus 1/2 inch (12 mm).

          - For location of elements in elevation, do not vary from that indicated by more than plus or minus 1/4 inch (6 mm) in a story height or 1/2 inch (12 mm) total.

        - Lines and Levels:

          - For bed joints and top surfaces of bearing walls, do not vary from level by more than 1/4 inch in 10 feet (6 mm in 3 m), or 1/2-inch (12-mm) maximum.

          - For conspicuous horizontal lines, such as lintels, sills, parapets, and reveals, do not vary from level by more than 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 1/2-inch (12-mm) maximum.

          - For vertical lines and surfaces, do not vary from plumb by more than 1/4 inch in 10 feet (6 mm in 3 m), 3/8 inch in 20 feet (9 mm in 6 m), or 1/2-inch (12-mm) maximum.

          - For conspicuous vertical lines, such as external corners, door jambs, reveals, and expansion and control joints, do not vary from plumb by more than 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 1/2-inch (12-mm) maximum.

          - For lines and surfaces, do not vary from straight by more than 1/4 inch in 10 feet (6 mm in 3 m), 3/8 inch in 20 feet (9 mm in 6 m), or 1/2-inch (12-mm) maximum.

        - Joints:

If using Type FBS Rough brick or Type FBA brick, revise tolerances in three subparagraphs below to allow for variation in brick size. Consider restricting tolerances if Type FBX brick is used.

          - For bed joints, do not vary from thickness indicated by more than plus or minus 1/8 inch (3 mm), with a maximum thickness limited to 1/2 inch (12 mm).

          - For head and collar joints, do not vary from thickness indicated by more than plus 3/8 inch (9 mm) or minus 1/4 inch (6 mm).

          - For exposed head joints, do not vary from thickness indicated by more than plus or minus 1/8 inch (3 mm).

      - LAYING MASONRY WALLS

        - Lay out walls in advance for accurate spacing of surface bond patterns with uniform joint thicknesses and for accurate location of openings, movement-type joints, returns, and offsets. Avoid using less-than-half-size units, particularly at corners, jambs, and, where possible, at other locations.

Pattern is usually running bond. If other bond patterns are required, specify in "Bond Pattern for Exposed Masonry" Paragraph below or indicate on Drawings.

        - Bond Pattern for Exposed Masonry: Unless otherwise indicated, lay exposed masonry in running bond; do not use units with less-than-nominal 4-inch (100-mm) horizontal face dimensions at corners or jambs.

        - Built-in Work: As construction progresses, build in items specified in this and other Sections. Fill in solidly with masonry around built-in items.

Revise first paragraph below if flexible perimeter joint or thermal break is required.

        - Fill space between steel frames and masonry solidly with mortar unless otherwise indicated.

        - Fill cores in hollow CMUs with grout 24 inches (600 mm) under bearing plates, beams, lintels, posts, and similar items unless otherwise indicated.

      - MASONRY-JOINT REINFORCEMENT

        - General: Install entire length of longitudinal side rods in mortar with a minimum cover of 5/8 inch (16 mm) on exterior side of walls, 1/2 inch (13 mm) elsewhere. Lap reinforcement a minimum of 6 inches (150 mm).

Revise three subparagraphs below if different spacing is required; delete if shown on Drawings.

          - Space reinforcement not more than 16 inches (406 mm) o.c.

          - Space reinforcement not more than 8 inches (203 mm) o.c. in foundation walls and parapet walls.

          - Provide reinforcement not more than 8 inches (203 mm) above and below wall openings and extending 12 inches (305 mm) beyond openings in addition to continuous reinforcement.

        - Interrupt joint reinforcement at control and expansion joints unless otherwise indicated.

First paragraph below can be deleted if rigid anchors are used to bond walls at intersections.

        - Provide continuity at wall intersections by using prefabricated T-shaped units.

        - Provide continuity at corners by using prefabricated L-shaped units.

      - ANCHORING MASONRY TO STRUCTURAL STEEL AND CONCRETE

        - Anchor masonry to structural steel and concrete, where masonry abuts or faces structural steel or concrete, to comply with the following:

          - Provide an open space not less than 1/2 inch wide between masonry and structural steel or concrete unless otherwise indicated. Keep open space free of mortar and other rigid materials.

          - Anchor masonry with anchors embedded in masonry joints and attached to structure.

          - Space anchors as indicated, but not more than 24 inches (610 mm) o.c. vertically and 36 inches (915 mm) o.c. horizontally.

      - FLASHING, WEEP HOLES, AND CAVITY VENTS

Retain option in "General" Paragraph below if wall is designed on rain-screen principle with cavity vents acting to equalize air-pressure differential between cavity and exterior. Indicate spacing of cavity vents and blocking on Drawings. See the Evaluations.

        - General: Install embedded flashing and weep holes in masonry at shelf angles, lintels, ledges, other obstructions to downward flow of water in wall, and where indicated. Install cavity vents at shelf angles, ledges, and other obstructions to upward flow of air in cavities, and where indicated.

        - Install flashing as follows unless otherwise indicated:

Retain option in first subparagraph below for manufactured flashing; delete if only metal flashing is used.

          - Prepare masonry surfaces so they are smooth and free from projections that could puncture flashing. Where flashing is within mortar joint, place through-wall flashing on sloping bed of mortar and cover with mortar. Before covering with mortar, seal penetrations in flashing with adhesive, sealant, or tape[ as recommended by flashing manufacturer].

Retain any of four subparagraphs below and revise to suit wall configurations used. Arrangement of flashing can be communicated better by detailing on Drawings rather than by relying on any of the nine subparagraphs.

          - At lintels and shelf angles, extend flashing a minimum of 6 inches (150 mm) into masonry at each end. At heads and sills, extend flashing 6 inches (150 mm) at ends and turn up not less than 2 inches (50 mm) to form end dams.

          - Install metal drip edges beneath flexible flashing at exterior face of wall. Stop flexible flashing 1/2 inch (13 mm) back from outside face of wall, and adhere flexible flashing to top of metal drip edge.

          - Install metal flashing termination beneath flexible flashing at exterior face of wall. Stop flexible flashing 1/2 inch (13 mm) back from outside face of wall, and adhere flexible flashing to top of metal flashing termination.

      - REINFORCED UNIT MASONRY INSTALLATION

Usually retain "Temporary Formwork and Shores" Paragraph below only if reinforced masonry beams, slabs, soffits, and similarly formed elements are required.

        - Temporary Formwork and Shores: Construct formwork and shores as needed to support reinforced masonry elements during construction.

          - Construct formwork to provide shape, line, and dimensions of completed masonry as indicated. Make forms sufficiently tight to prevent leakage of mortar and grout. Brace, tie, and support forms to maintain position and shape during construction and curing of reinforced masonry.

          - Do not remove forms and shores until reinforced masonry members have hardened sufficiently to carry their own weight and that of other loads that may be placed on them during construction.

        - Placing Reinforcement: Comply with requirements in TMS 602/ACI 530.1/ASCE 6.

        - Grouting: Do not place grout until entire height of masonry to be grouted has attained enough strength to resist grout pressure.

          - Comply with requirements in TMS 602/ACI 530.1/ASCE 6 for cleanouts and for grout placement, including minimum grout space and maximum pour height.

Retain subparagraph below unless high-lift grouting is allowed. See the Evaluations. TMS 602/ACI 530.1/ASCE 6 limits grout lifts to 60 inches (1520 mm) unless masonry has cured for at least 4 hours, grout slump is between 10 and 11 inches (254 and 279 mm), and there are no intermediate bond beams between top and bottom of pour height.

          - Limit height of vertical grout pours to not more than 60 inches (1520 mm).

      - FIELD QUALITY CONTROL

        - Testing and Inspecting: Owner will engage special inspectors to perform tests and inspections and prepare reports. Allow inspectors access to scaffolding and work areas as needed to perform tests and inspections. Retesting of materials that fail to comply with specified requirements shall be done at Contractor's expense.

Level B special inspections are required for masonry in nonessential facilities designed by either analytical method and for essential facilities designed by empirical method; Level C for masonry in essential facilities (IBC Occupancy Category IV) designed by either analytical method.

        - Inspections: Special inspections according to Level [B] [C] in TMS 402/ACI 530/ASCE 5.

Revise subparagraphs below to suit level of inspection required, based on occupancy category and design method.

          - Begin masonry construction only after inspectors have verified proportions of site-prepared mortar.

          - Place grout only after inspectors have verified compliance of grout spaces and of grades, sizes, and locations of reinforcement.

          - Place grout only after inspectors have verified proportions of site-prepared grout.

Retain "Testing Prior to Construction" Paragraph below for masonry in nonessential facilities designed by either analytical method and for essential facilities designed by empirical method.

        - Testing Prior to Construction: One set of tests.

Testing frequency in "Testing Frequency" Paragraph below is requirement for masonry in essential facilities (IBC Occupancy Category IV) designed by either analytical method.

        - Testing Frequency: One set of tests for each 5000 sq. ft. (464 sq. m) of wall area or portion thereof.

Retain "Clay Masonry Unit Test" and "Concrete Masonry Unit Test" paragraphs below, as applicable, if unit-strength method is used. Delete both paragraphs if retaining prism-test method.

        - Clay Masonry Unit Test: For each type of unit provided, according to ASTM C 67 for compressive strength.

        - Concrete Masonry Unit Test: For each type of unit provided, according to ASTM C 140 for compressive strength.

TMS 402/ACI 530/ASCE 5 requires verification of compliance of proportions for site-prepared mortar. Mortar aggregate ratio test in "Mortar Aggregate Ratio Test (Proportion Specification)" Paragraph below verifies ratio of aggregate to cementitious materials but does not indicate what cementitious materials are used. Observation of actual mortar mixing procedures as part of inspection program would provide better quality control.

        - Mortar Aggregate Ratio Test (Proportion Specification): For each mix provided, according to ASTM C 780.

"Mortar Test (Property Specification)" Paragraph below may be deleted if mortar is specified to comply with proportion specification or if retaining prism test. Testing for mortar air content is especially desirable for reinforced masonry. Testing for compressive strength is required if the property specification for mortar is used. Note that ASTM C 780 states, "Strength values for mortars obtained through these testing procedures are not required, nor expected, to meet strength requirements of laboratory Specification C 270 mortars."

        - Mortar Test (Property Specification): For each mix provided, according to ASTM C 780. Test mortar for [mortar air content] [and] [compressive strength].

"Grout Test (Compressive Strength)" Paragraph below may be deleted if grout is specified by proportions stated in ASTM C 476 rather than by compressive strength or if retaining prism test.

        - Grout Test (Compressive Strength): For each mix provided, according to ASTM C 1019.

      - REPAIRING, POINTING, AND CLEANING

        - In-Progress Cleaning: Clean unit masonry as work progresses by dry brushing to remove mortar fins and smears before tooling joints.

        - Final Cleaning: After mortar is thoroughly set and cured, clean exposed masonry as follows:

          - Remove large mortar particles by hand with wooden paddles and nonmetallic scrape hoes or chisels.

          - Test cleaning methods on sample wall panel; leave one-half of panel uncleaned for comparison purposes.

Delete first two subparagraphs below if cleaners are not specified in Part 2 or if cleaners are not allowed.

          - Protect adjacent surfaces from contact with cleaner.

          - Wet wall surfaces with water before applying cleaners; remove cleaners promptly by rinsing surfaces thoroughly with clear water.

          - Clean brick by bucket-and-brush hand-cleaning method described in BIA Technical Notes 20.

Retain either or both of last two subparagraphs above, or retain first subparagraph below. Coordinate with products retained in Part 2. If high-pressure water cleaning or other methods are acceptable, delete or revise subparagraph below and insert applicable requirements.

          - Clean masonry with a proprietary acidic cleaner applied according to manufacturer's written instructions.

      - MASONRY WASTE DISPOSAL

Retain "Waste Disposal as Fill Material" Paragraph below if clean masonry waste can be used as fill in footing trenches, etc. This diverts some material from waste stream, conserving landfill space and energy required to haul waste away.

        - Waste Disposal as Fill Material: Dispose of clean masonry waste, including excess or soil-contaminated sand, waste mortar, and broken masonry units, by crushing and mixing with fill material as fill is placed.

Generally retain subparagraph below. If required, increase limit if acid-soil plants are used for foundation plantings.

          - Do not dispose of masonry waste as fill within 18 inches (450 mm) of finished grade.

        - Masonry Waste Recycling: Return broken CMUs not used as fill to manufacturer for recycling.

        - Excess Masonry Waste: Remove excess clean masonry waste that cannot be used as fill, as described above or recycled, and other masonry waste, and legally dispose of off Owner's property.

END OF SECTION 042000