Copyright 2016 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 061000 - ROUGH CARPENTRY

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

- GENERAL

<Double click here to submit questions, comments, or suggested edits to this section.>

      - SUMMARY

        - Section Includes:

          - Framing with dimension lumber.

          - Framing with engineered wood products.

          - Shear wall panels.

          - Rooftop equipment bases and support curbs.

          - Wood blocking and nailers.

          - Wood furring.

          - Wood sleepers.

          - Plywood backing panels.

- PRODUCTS

Manufacturers and products listed in SpecAgent and Masterworks Paragraph Builder are neither recommended nor endorsed by the AIA or ARCOM. Before inserting names, verify that manufacturers and products listed there comply with requirements retained or revised in descriptions and are both available and suitable for the intended applications. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - WOOD PRODUCTS, GENERAL

        - Lumber: DOC PS 20 and applicable rules of grading agencies indicated. If no grading agency is indicated, comply with the applicable rules of any rules-writing agency certified by the ALSC Board of Review. Grade lumber by an agency certified by the ALSC Board of Review to inspect and grade lumber under the rules indicated.

          - Factory mark each piece of lumber with grade stamp of grading agency.

Retain only first option in first subparagraph below if authorities having jurisdiction require grade stamps on all materials.

          - For exposed lumber indicated to receive a stained or natural finish, mark grade stamp on end or back of each piece or omit grade stamp and provide certificates of grade compliance issued by grading agency.

Revise subparagraph below if rough lumber is acceptable for all work.

          - Dress lumber, S4S, unless otherwise indicated.

Retain one of three options in "Maximum Moisture Content of Lumber" Paragraph below, or delete paragraph if green lumber is acceptable in all thicknesses. Verify availability of lumber with 15 percent maximum moisture content before retaining. Lumber more than 2 inches nominal (38 mm actual) in thickness is often shipped green. See the Evaluations.

        - Engineered Wood Products: Acceptable to authorities having jurisdiction and for which current model code research or evaluation reports exist that show compliance with building code in effect for Project.

          - Allowable design stresses, as published by manufacturer, shall meet or exceed those indicated. Manufacturer's published values shall be determined from empirical data or by rational engineering analysis and demonstrated by comprehensive testing performed by a qualified independent testing agency.

      - WOOD-PRESERVATIVE-TREATED LUMBER

        - Preservative Treatment by Pressure Process: AWPA U1; Use Category UC2 for interior construction not in contact with ground, Use Category UC5a for exterior construction not in contact with ground, and Use Category UC5a for items in contact with ground.

See the Evaluations for information about treatment chemicals.

          - Preservative Chemicals: Acceptable to authorities having jurisdiction and containing no arsenic or chromium.

        - Kiln-dry lumber after treatment to a maximum moisture content of 19 percent. Do not use material that is warped or that does not comply with requirements for untreated material.

        - Mark lumber with treatment quality mark of an inspection agency approved by the ALSC Board of Review.

Retain first option in "Application" Paragraph below and delete list that follows if all rough carpentry must be treated with wood preservative. Coordinate paragraph and list with requirements for fire-retardant-treated materials; wood cannot be both preservative treated and fire-retardant treated.

        - Application: Treat all rough carpentry unless otherwise indicated.

Retain first subparagraph below if Project includes wood adjacent to roofing or waterproofing.

          - Wood cants, nailers, curbs, equipment support bases, blocking, stripping, and similar members in connection with roofing, flashing, vapor barriers, and waterproofing.

          - Wood sills, sleepers, blocking, furring, stripping, and similar concealed members in contact with masonry or concrete.

          - Wood framing and furring attached directly to the interior of below-grade exterior masonry or concrete walls.

          - Wood framing members that are less than 18 inches (460 mm) above the ground in crawlspaces or unexcavated areas.

          - Wood floor plates that are installed over concrete slabs-on-grade.

Insert other items that require treatment but are not likely to be indicated on Drawings.

      - DIMENSION LUMBER FRAMING

"Non-Load-Bearing Interior Partitions" and "Framing Other Than Non-Load-Bearing Partitions" paragraphs below provide choices for specifying different categories of framing.

        - Framing Other Than Non-Load-Bearing Partitions: No. 2

          - Application: Framing other than interior partitions].

          - Species:

Usually retain all species below that meet requirements except those unavailable in Project's location. Species groups are listed in order of decreasing strength (extreme fiber in bending).

            - Douglas fir-larch; WCLIB or WWPA.

Delete "Southern pine; SPIB" Subparagraph above if retaining first subparagraph below.

            - \Exposed Framing: Hand-select material for uniformity of appearance and freedom from characteristics, on exposed surfaces and edges, that would impair finish appearance, including decay, honeycomb, knot-holes, shake, splits, torn grain, and wane.

          - Species and Grade: As indicated above for load-bearing construction of same type.

      - SHEAR WALL PANELS

        - Wood-Framed Shear Wall Panels: Prefabricated assembly consisting of wood perimeter framing, tie downs, and Exposure I, Structural I plywood or OSB sheathing.

        - Allowable design loads, as published by manufacturer, shall meet or exceed those indicatedManufacturer's published values shall be determined from empirical data or by rational engineering analysis and demonstrated by comprehensive testing performed by a qualified independent testing agency.

      - MISCELLANEOUS LUMBER

        - General: Provide miscellaneous lumber indicated and lumber for support or attachment of other construction, including the following:

          - Blocking.

          - Nailers.

          - Rooftop equipment bases and support curbs.

          - Cants.

          - Furring.

          - Grounds.

        - Dimension Lumber Items: Construction or No. 2 grade lumber of any species.

Retain "Concealed Boards" Paragraph below for furring, grounds, and nailing strips if required, and for truss bracing specified by referencing this Section.

        - Concealed Boards: 19 percent maximum moisture content.

      - FASTENERS

        - General: Fasteners shall be of size and type indicated and shall comply with requirements specified in this article for material and manufacture.

          - Where rough carpentry is exposed to weather, in ground contact, pressure-preservative treated, or in area of high relative humidity, provide fasteners Type 304 stainless steel.

        - Power-Driven Fasteners: Fastener systems with an evaluation report acceptable to authorities having jurisdiction, based on ICC-ES AC70.

ICC-ES AC01 and ICC-ES AC193 are for mechanical anchors in masonry and concrete respectively, ICC-ES AC58 and ICC-ES AC308 are for adhesive anchors in masonry and concrete.

      - MISCELLANEOUS MATERIALS

Retain one of two "Sill-Sealer Gaskets" paragraphs below if required. First paragraph is suitable for dry masonry. Second paragraph is more suitable for applications close to the ground or likely to remain damp.

        - Sill-Sealer Gaskets: Glass-fiber-resilient insulation, fabricated in strip form, for use as a sill sealer; 1-inch (25-mm) nominal thickness, compressible to 1/32 inch (0.8 mm); selected from manufacturer's standard widths to suit width of sill members indicated.

        - Sill-Sealer Gaskets: Closed-cell neoprene foam, 1/4 inch (6.4 mm) thick, selected from manufacturer's standard widths to suit width of sill members indicated.

Retain "Flexible Flashing" Paragraph below if required as a separator between preservative-treated wood and metal decking.

        - Flexible Flashing: Composite, self-adhesive, flashing product consisting of a pliable, butyl rubber or rubberized-asphalt compound, bonded to a high-density polyethylene film, aluminum foil, or spunbonded polyolefin to produce an overall thickness of not less than 0.025 inch (0.6 mm).

        - Adhesives for Gluing to Concrete or Masonry: Formulation complying with ASTM D 3498 that is approved for use indicated by adhesive manufacturer.

- EXECUTION

      - INSTALLATION, GENERAL

        - Framing Standard: Comply with AF&PA's WCD 1, "Details for Conventional Wood Frame Construction," unless otherwise indicated.

        - Framing with Engineered Wood Products: Install engineered wood products to comply with manufacturer's written instructions.

        - Set rough carpentry to required levels and lines, with members plumb, true to line, cut, and fitted. Fit rough carpentry accurately to other construction. Locate nailers, blocking, and similar supports to comply with requirements for attaching other construction.

        - Install shear wall panels to comply with manufacturer's written instructions.

        - Install metal framing anchors to comply with manufacturer's written instructions. Install fasteners through each fastener hole.

        - Do not splice structural members between supports unless otherwise indicated.

        - Comply with AWPA M4 for applying field treatment to cut surfaces of preservative-treated lumber.

        - Where wood-preservative-treated lumber is installed adjacent to metal decking, install continuous flexible flashing separator between wood and metal decking.

        - Securely attach rough carpentry work to substrate by anchoring and fastening as indicated, complying with the following:

Retain one of first two subparagraphs below, as required to comply with requirements of Project and local codes.

          - Table 2304.9.1, "Fastening Schedule," in ICC's International Building Code (IBC).

          - Table R602.3(1), "Fastener Schedule for Structural Members," and Table R602.3(2), "Alternate Attachments," in ICC's International Residential Code for One- and Two-Family Dwellings.

          - ICC-ES evaluation report for fastener.

      - PROTECTION

Delete this article if site-applied boron treatment is specified in Section 313116 "Termite Control."

        - Protect wood that has been treated with inorganic boron (SBX) from weather. If, despite protection, inorganic boron-treated wood becomes wet, apply EPA-registered borate treatment. Apply borate solution by spraying to comply with EPA-registered label.

Retain paragraph below if borate treatment of wood that has become wet is used to help prevent mold and mildew.

        - Protect rough carpentry from weather. If, despite protection, rough carpentry becomes wet, apply EPA-registered borate treatment. Apply borate solution by spraying to comply with EPA-registered label.

END OF SECTION 061000